we present a

simple and rationale design of the UCNPs’ surface that ensures

their protection in aqueous media under different harsh conditions.

Our approach is based on the combination of two

synergic strategies: first, the oleic acid ligands at the surface

of UCNPs are replaced in nonpolar solvents by 10-methacryloyldecylphosphate

(MDP), to achieve surface passivation, colloidal

stability in organic media, and a terminal polymerizable

group. Second, the dispersion and free-radical miniemulsion

polymerization of these UCNPs in styrene (St), or a mixture

of St and methyl methacrylate (MMA), pursues the formation

of a robust hydrophobic shell of controlled thickness that insulates

and protects UCNPs from aqueous environment. This

method is also expected to provide them with colloidal stability

in aqueous media due to the presence of polar groups incorporated

during the polymerization process.

The stunning optical properties of upconverting nanoparticles (UCNPs) have

inspired promising biomedical technologies. Nevertheless, their transfer to

aqueous media is often accompanied by intense luminescence quenching,

partial dissolution by water, and even complete degradation by molecules such

as phosphates. Currently, these are major issues hampering the translation

of UCNPs to the clinic. In this work, a strategy is developed to coat and

protect β-NaYF4 UCNPs against these effects, by growing a hydrophobic

polymer shell (HPS) through miniemulsion polymerization of styrene (St), or

St and methyl methacrylate mixtures. This allows one to obtain single core@

shell UCNPs@HPS with a final diameter of ≈60–70 nm. Stability studies

reveal that these HPSs serve as a very effective barrier, impeding polar

molecules to affect UCNPs optical properties. Even more, it allows UCNPs

to withstand aggressive conditions such as high dilutions (5 μg mL−1), high

phosphate concentrations (100 mm), and high temperatures (70 °C). The

physicochemical characterizations prove the potential of HPSs to overcome

the current limitations of UCNPs. This strategy, which can be applied to other

nanomaterials with similar limitations, paves the way toward more stable and

reliable UCNPs with applications in life sciences.

LiYF4:20Yb2Er@LiYF4

L

NaYF4:20Yb2Er

NaHoW@NaGdW:20Yb1Tm

NaHoW@NaGdW;20Yb:1Tm@NaGdW:20Yb:20Nd